衝擊撓度指標應用於剛性鋪面殘餘壽年之預測

The method of the data interpretations of the nondestructivedeflection tests can devided into two ways: deflection index methodand stress analysis method. Because the deflection index method isless time consuming and more convenient than the other method, so itis popularly used by the engineers. This study is, thereby, motivatedto develop impulsive deflection for the rigid pavement, and also findout regression formula between the deflection index and pavementstrength, According to the combination of regression formula and theAASHTO design guide, in which the ESAL value is compared, engineerscan get the in-situ pavement strength and the remaining life to offerthe maintenance strategies.