公車專用道面層材料改善之研究

With the heavy carrying capacity and amounts of runs of scheduledbuses, the bus lanes are seriously damaged that cause distress, suchas rutting, and deformation. In addition, the hot and wet weather ofTaipei basin has led the moisture into the bus lanes, that makes thestripping of bus lanes' surface course materials. Working withMarshall Mixture Design Analysis and SMA Mixture Design AnalysisMethod to decide optimum recommended asphalt content, the study adoptsasphalt, 3/8", 3/4" DGAC of bus lanes' surface course materials inTaipei, and other materials to make samples. Being cooperating withfield sample tests, mechanics tests, performance tests and strippingtests were done by these samples in the study to know the evaluationof performance of bus lanes brought by different combination ofasphalt. One brief comparison of different policies' capitalevaluation is furthermore done to see if they are economic and providesome information to the future studies.