自行架橋型之硫化聚胺酯的合成應用與性質探討

In this research, a cross self-curing system of polythiourethane was the main target. The five-membered dithiocarbonate was obtained from the epoxy-rings (DGEBA) which reated with carbon disulfide(CS2). Furthermore, the dithiocarbonate reacted with various diamines (Jeffamine D-2000, PDMS-diamine) to give the products, poly(thiolthiourethanes), and the S-S bonds produced by the auto-oxidation of pendant thiol group.