功能性高分子的應用與開發

We use UV-curing technology, Moisture curing system and Electron Beam radiation on textile functional treatment. Series of functional coating system were established via synthesis novel polymer materials. Fluorinated polymer mix with UV-curable epoxy, or treated via electron beam irradiation process can effectively enhance the durability of water repellent coating, and with IPN system, UV-curable or Moisture curable PDMS containing PU could formed a long lasting water repellent coating on textile. The contact angle on optimum treated textile can reach 150 and remain the same after 50 washing cycles.