Electrical properties of the GDC oxide and GDC carbonate composite

L.C. Wen1, Y.I. Tsai2, H.K. Lin3, S.C. Chang4, H.-C.I. Kao5*, H.S. Sheu6, M.C. Lee7, Y.S. Lee8

1-5Department of Chemistry, Tamkang University, Tamsui, Taiwan 25137

6National Synchrotron Radiation Research Center, Hsinchu, Taiwan 30076

7,8Institute of Nuclear Energy Research, Atomic Energy Council, Longtan, Taiwan 32546

Tel: (02)26215656 ext. 2547, Email: kaohci@gmail.com

5-8Professor, 1Graduate student, 2-4Undergraduate student, *Corresponding author

Abstract

A GDC-composite was prepared by immersion porous (Ce0.8Gd0.2)O1.9 having a relative density around 65‒70% into molten mixture of carbonates containing 1:1 molar ratio of Li2CO3 and Na2CO3 at 500(C for 12 h. Relative density of the composite is close to 100%. In addition, dense GDC oxide without carbonates was heat treated at 1500(C that had a relative density near 100% too. At 500(C, electrical conductivity and the ionic transference number (ti) of the GDC oxide is 1.54 x 10(3 S(cm(1 and 0.994, respectively, electronic conduction can be neglected. Increasing temperature, ti of GDC decreases gradually. Adding carbonates into GDC, electrical conductivity reaches to 1.04 x 10(1 S(cm(1 at 500(C.  Measuring electrical conductivity of the GDC( composite at 490(C, after 17 days (400 h), it becomes 5.93(3) x 10(2 S(cm(1 and leveling off. GDC(composite is a potential electrolyte material to be used in the solid oxide fuel cell (SOFC) at temperature lower than 500(C.

Keywords: GDC; Composite; Conductivity; SOFC; Carbonate

1. Introduction

Solid oxide fuel cells (SOFCs) have been developed rapidly in recent years due to their all solid state component which broadens the application potential. SOFC is a highly efﬁcient power generation system due to its several advantages, such as fuel ﬂexibility and reduced pollution, etc. In general, SOFC framework is based on a sandwiched structure, including dense electrolyte of 8YSZ between two porous electrodes, such as the anode (Ni–YSZ) and the cathode (La1−xSrxMnO3) [1(5].

The commercially available solid electrolyte (8YSZ) is usually operated at temperatures as high as 800( 1000(C to obtain the required high ionic conductivity. It may cause the reaction between components of the modules. Thermal degradation or thermal expansion would restrict the fabrication of the SOFCs [6].

Nowadays, reducing the operation temperature of SOFCs to 300(600(C is tremendously interested because it improves material compatibility effectively, reduces the fabricating cost and prolongs the operating lifetime. Many researchers are attracted to the rare earth doped ceria based (RDC) multi-phase electrolytes due to their excellent performance at lower temperatures (300(600(C) [7]. For example, Zhu et al. studies many composites, such as, GDC(NaCl, GDC(NaOH, GDC(MCO3 (M = Ca, Ba and Sr), SDC(M2CO3 (M = Li, Na and K) [7]. Especially, the SDC(Na2CO3 composite has the power density of 200(1150 mW(cm2 at 300(600(C. The excellent performance was explained by an interfacial conduction mechanism in the two-phase region which was called the superionic phase. Electronic conduction caused by the reduction of the Ce4+ to Ce3+ above 500(C at hydrogen atmosphere can be suppressed effectively by using the operation temperature to 500(C or below [8]. Zhu et al. has also studied the conductivity of the SDC carbonate (Li0.62K0.38CO3) composite as a function of the carbonate volume fraction. Conductivity reaches to an optimum with carbonate volume fraction over 30 v%.

Conductivity of the composite is not only contributed by the O2(, but also by the CO32( and H+. The percentage of the O2(, CO32( and H+ ion conduction measured by EMF (electromotive force) at 500(C are 31%, 67% and 2% and they are 24%, 67% and 9% at 550(C, respectively [9]. By using the Hebb(Wagner’s ion- blocking cell to measure the electronic contribution of the SDC(composite in the temperature range, 500( 550(C, it was 10(4 S·cm(1 and about 0.1% of the total conductivity so that it is negligible [9(12].

The oxide carbonate composites were generally prepared by mixing appropriate amount of oxides and carbonates through ball milling or coprecipitation method. Mixture was sintered by 600(750(C for 0.5(1 h [2,13(15]. This temperature is higher than the decomposing temperature of the 1:1 molar ratio of the Li2CO3 and Na2CO3 mixture. On the other hand, relative density of the composite is probably not dense enough due to the low sintering temperature and short heating period. In this report, different preparation process is employed to avoid the decomposition of the carbonates and to guarantee the obtained GDC carbonate composite is dense enough for using as an electrolyte material.

2. Experimental

Appropriate amount of 99.9% of Gd2O3 (Strem), 99.9% of CeO2 (Strem), Li2CO3 (Merck), Na2CO3 (Merck) and PMMA (poly(methyl methacrylate)) were employed to prepare composite samples in this report. Gd2O3 and CeO2 were weighed and ball milled for 24 h with zirconia balls in acetone for making precursor GDC oxide powder, which was heat treated at 1500°C for 5 h to prepare dense oxide or at 1000(C for 10 h to prepare porous material. 1:1 molar ratio of the Li2CO3 and Na2CO3 (LNCO) mixture was ball milled for 24 h. Porous GDC sample is covered by molten LNCO at 500°C for 12 h to allow the carbonates to penetrate into the channels of the porous sample.

Relative density of the sintered specimens was measured by the Archimedes method using de-ionized water as a liquid medium, but the porous sample was measured by geometry method. Powder diffraction data used for the Rietveld refinement were collected on the BL01C2 beam line at the National Synchrotron Radiation Research Center (NSRRC) in Taiwan. The GSAS (General Structure Analysis System) program developed by Larson and von Dreele was employed for the structural parameters analysis with the Rietveld method [16]. Morphology of the sample was observed with a VEGA\\SBH Scanning Electron Microscope.

Electrical parameters were determined by the AC impedance spectroscopy (EIS) using a fully automated Autolab PGSTAT30 Potentiostat/Galvanostat system in air in the frequency range from 1 MHz to 1 Hz with a density of 10 points/decade and the excitation amplitude of 50 mV in the temperature range from 300 to 700°C. Pellet samples were measured by a 2-probe method with Pt electrodes and Ag paste. An K-type thermocouple was attached near the sample to measure the temperature. Electromotive forces (EMFs) were measured on an oxygen concentration cell, in which ambient air was employed as a reference and a mixed gas, oxygen and argon, was introduced to another side of the cell. The flow rate were fixed by a mass flow controller to a total rate of 100 sccm. The whole system was allowed to stabilize under each condition before the measurement [17,18].

3. Results and Discussion

XRD patterns of the GDC and GDC(composite are shown in Fig. 1. Small diffraction peaks of Li2CO3 and Na2CO3 are marked in the Fig. Their diffraction angles (2θ) calculated with a wavelength of 0.0495941 nm are listed in Table 1. The peaks belonging to the GDC and GDC(composite are exactly the same that is not influenced by the coexistence of the carbonates. No reaction happens between oxide and carbonates.

Rietveld refinement result of the GDC oxide is shown in Fig. 2. Crosses show the experimental data; solid lines are the calculated profiles. All the possible Bragg diffractions are indicated with short vertical tics below the calculated profiles. The difference between the experimental and calculated results is plotted below the Bragg diffraction tics. Some refinement results are listed in Table 2, the Rwp and Rp obtained are 3.62 and 1.32%, respectively, and the (2 is 3.415. All of them are acceptable and the results are believable. Unit cell a-axis is 5.4237(6) Å. GDC has a fluorite phase.

Morphology of the GDC oxide sintered at 1500(C, 1000(C and GDC(composite are shown in Fig. 3. The SEM images were taken on a cross section area of the bulk samples. The pure GDC oxide sintered at 1500(C reaches to 99.4% relative density is shown in Fig. 3(a). In order to have more than 30% carbonated volume fraction in composite, porous GDC oxide was prepared by lowering sintering temperature to 1000(C, and then allowed the liquefied LNCO carbonates to penetrate into the open channels at 500(C. Relative density of the porous GDC oxide is 67.4% shown in Fig. 3(b) and the dense composite has a relative density of 99.6(2)% shown in Fig. 3(c). Relative densities of all samples are listed in Table 3.

Typical impedance Cole(Cole plots (Nyquist diagrams) for all samples were obtained by a 2-probe configuration, Pt(sample(Pt, in the ambient pressure. The impedance data of the GDC oxide is interpreted by using an equivalent circuit model of a series connection form (Rg//Cg)(Rgb//Cgb)Ce shown in Fig. 4, where the symbols of g and gb represent grain and grain boundary, respectively. The symbols of R and C in parallel represent the corresponding resistance and the universal capacitance in each contribution [19]. In the impedance plot, the bulk resistance (Rg) appears in the higher frequency semicircle on the left hand side, and the grain boundary resistance (Rgb) is in the lower frequency one on the right hand side. The total resistance is the summation of the grain and grain boundary resistances. The impedance data of the GDC(composite is interpreted by using an equivalent circuit model of a series connection form Rb(Re//Ce)(Re/e//Ce/e) shown in Fig. 5, where the symbols of b, e and e/e represent the bulk sample, electrode and the interface between electrode and electrolyte, respectively. The total resistance is only the bulk sample (Rb) resistance [1].

Fig. 6 is the Arrhenius plots of the GDC oxide and GDC(composite. The GDC oxide obeys the Arrhenius equation well, indicating that the ionic diffusion process is thermally activated [20]. The correlation values (R2) found for the GDC oxide is 0.9976, quite close to 1. The Arrhenius plot of the GDC(composite has three distinct stages including the lower temperature range, approaching and over the melting point (m.p.) of the carbonates. Activation energies for all the sample at different temperature regions are listed in Table 4. In the low temperature region, Ea of the composite is higher than that of the pure oxide. Carbonates contribution to the electrical conduction is apparent. In the medium temperatures, carbonates are approaching their melting point, mobility is greatly increased, Ea increases further. At this stage, the GDC(composite has a conductivity 2‒3 orders of magnitude higher than that of the GDC oxide. In the high temperature region, carbonates are in the liquid state, activation energy is still required for the electrical transportation. Nevertheless, Ea is small. Electrical conductivity (() of the (Ce0.8Gd0.2)O1.9( composite reaches to 10(1 S(cm(1, which is high enough for an electrolyte.

Fig. 7 shows a long-term stability test of the ( of the GDC(composite at 490(C. The LNCO melts at about 495(C [13‒15] so that the stability test is running at 490(C and hope that the carbonates are always in solid state. Initially, ( decreases fast, from 0.11 to 0.067 S(cm(1 after 1 d test and then, ( levels off to 0.057 ( 0.02 S(cm(1 from ea. 100 to 400 h. At this temperature, no electrolyte does probably flow away so that ( is kept to a constant. Although the conductivity is slightly smaller than 10(1 S(cm(1, GDC(composite is still a potential electrolyte material being used in the SOFCs at 490(C.

4. Conclusions

Fully dense GDC(composite was prepared by immersion porous oxide into molten mixture of carbonates and the relative density of the composite is close to 100%, which has electrical conductivity in the 10(1 S(cm(1 range at 500(C. After long term stability test, ( reaches to about 0.06 S(cm(1 at 490(C. In order to use it at solid state, ( would be slightly sacrificed.

5. Acknowledgments

This work is financially supported by the Institute of Nuclear Energy Research, Atomic Energy Council of Taiwan under the contract number 1012001INER039.

6. References

[1] Zhang, L., Lan, R., Petit, C. T. G., Tao, S., 2010, “Durability study of an intermediate temperature fuel cell based on an oxide-carbonate composite electrolyte,” International Journal of Hydrogen Energy, Vol. 35, No. 13, pp. 6934-6940.

[2] Xia, Y., Bai, Y., Wu, X., Zhou, D., Liu, X., Meng, J., 2011, “The competitive ionic conductivities in functional composite electrolytes based on the series of M-NLCO (M = Ce0.8Sm0.2O2-δ, Ce0.8Gd0.2O2-δ, Ce0.8Y0.2O2-δ; NLCO = 0.53Li2CO3-0.47Na2CO3),” International Journal of Hydrogen Energy, Vol. 36, pp. 6840-6850.

[3] Lara, C., Pascual, M. J., Duran, A., 2007, “Phase separation in metastable glasses under microgravity conditions,” Journal of Glass Science and Technology Part B, Vol. 48, pp. 218-224.

## [4] Brandon, N. P., Skinner, S., Steele, B. C. H., 2003,

## “Recent advances in materials for fuel cells,” Annual

## Review of Materials Research, Vol. 33, pp. 183-213.

## [5] Orera, A., Slater, P. R., 2010, “New Chemical Systems for Solid Oxide Fuel Cells,” Chemical of Materials, Vol. 22, pp. 675-690.

[6]  Su, X. T., Yan, Q. Z., Ma, X. H., Zhang, W. F., Ge, C. C., 2006, “Effect of co-dopant addition on the properties of yttrium and neodymium doped barium cerate electrolyte,” Solid State Ionics, Vol. 177, pp. 1041-1045.

[7]  Zhu, B., Li, S., Mellander, B. E., 2008, “Theoretical approach on ceria-based two-phase electrolytes for low temperature (300-600(C) solid oxide fuel cells,” Electrochemistry Communication, Vol. 10, pp. 302-305.

[8]  Wang, X. D., Ma, Y., Raza, R., Muhammed, M., Zhu, B., 2008, “Novel coreeshell SDC/amorphous Na2CO3 nanocomposite electrolyte for low-temperature SOFCs,” Electrochemistry Communication, Vol. 10, pp. 1617-1620.

[9]  Zhu, W., Xia, C., Ding, D., Shi, X., Meng, G., 2006, “Electrical properties of ceria-carbonate composite electrolytes,” Materials Research Bulletin, Vol. 41, pp. 2057-2064.

[10] Xiong, Y. P., Yamaji, K., Sakai, N., Negishi, H., Horita, T., Yokokawa, H., 2001, “Electronic Conductivity of ZrO2-CeO2-YO1.5 Solid Solutions,” Journal of The Electrochemical Society,” Vol. 148, pp. 489-493.

## [11] Zhang, L., Lan, R., Petit, C. T. G., Tao, S., 2010, “Durability study of an intermediate temperature fuel cell based on an oxide-carbonate composite electrolyte,” International Journal of Hydrogen Energy, Vol. 35, No. 13, pp. 6934-6940.

## [12] Keen, D. A., 2002, “Disordering phenomena in superionic conductors,” Journal of Physics: Condensed Matter, Vol. 14, pp. 189.

## [13] Zhu, B., Raza, R., Qin, H., Fan, L., 2011, “Single-component and three-component fuel cells,” Journal of Power Sources, Vol. 196, No. 15, pp. 6362-6365.

## [14] Gao, Z., Raza, R., Zhu, B., Mao, Z., Wang, C., Liu, Z., 2011, “Preparation and characterization of Sm0.2Ce0.8O1.9/Na2CO3 nanocomposite electrolyte for low-temperature solid oxide fuel cells,” International Journal of Hydrogen Energy, Vol. 36, pp. 3984-3988.

## [15] Chockalingam, R., Basu, S., 2011, “Impedance spectroscopy studies of Gd-CeO2-(LiNa)CO3 nano composite electrolytes for low temperature SOFC applications,” International Journal of Hydrogen Energy, Vol. 36, pp. 14977-14983.

## [16] Larson, A. C., von Dreele, R. B., 2003, General Structure Analysis System; Report La-UR-86-748; Los Alamos National Laboratory, Los Alamos, NM, USA.

## [17] West A.R., 1999, Basic Solid State Chemistry, 2nd ed., Wiley, New York, USA, pp. 351-352.

## [18] West A.R., 1999, Basic Solid State Chemistry, 2nd ed., Wiley, New York, USA, pp. 357-361.

[19] Díaz-Guillén, J. A., Díaz-Guillén, M. R., Padmasree, K. P., Fuentes, A. F., Santamaría, J., León, C., 2008, “High ionic conductivity in the pyrochlore-type Gd2-yLayZr2O7 solid solution (0≤y≤1),” Solid State Ionics, Vol. 179, pp. 2160-2164.

[20] Liu, Z. G., Ouyang, J. H., Sun, K. N., Xia, X. L., 2010, “Effect of Gd and Yb co-doping on structure and electrical conductivity of the Sm2Zr2O7 pyrochlore,” Vol. 195, pp. 7225-7229.

8. Figures and Tables

Fig. 1. XRD patterns of the (a) GDC and (b) GDC( composite, wavelength of the X(ray beam is 0.15418 nm (top) and 0.0495941 nm (bottom).

Fig. 2. Rietveld refinement results of the GDC. The figures include the experimental, calculated, and difference XRD profiles. Crosses are the experi- mental data; solid lines are the calculated profile. All the possible Bragg reflections are indicated with short vertical tics below the calculated profile. The difference between the experimental and calculated results is plotted below the Bragg refraction tics.

Fig.3. SEM patterns of the (a) GDC sintered at 1500(C for 10 h, (b) GDC sintered at 1000(C for 10 h and (c) GDC(composite prepared at 500(C for 12 h. All the images are in 5000 magnification.

Fig. 4. Complex impedance plots obtained at (■) 500(C,

(●) 525(C and (▲) 552(C for the GDC. The equivalent circuit model is shown in the figure.

Fig. 5. Complex impedance plots obtained at (■) 375(C,

(●) 400(C and (▲) 435(C for the GDC(composite. The equivalent circuit model is shown in the figure.

Fig. 6. Arrhenius plots of the total conductivity of the (■) GDC and (□) GDC(composite.

Fig. 7. Stability of the electrical conductivity of the

GDC( composite at 490(C.

Table 1 Five main XRD peaks of the Li2CO3 and Na2CO3 (Wavelength of the X-ray beam is 0.0495941 nm.)

| Li2CO3 | Na2CO3 |
| --- | --- |
| 6.9o | 8.6o |
| 9.9o | 10.7o |
| 10.2o | 11.1o |
| 11.0o | 13.6o |
| 11.9o | 15.7o |

Table 2 Unit cell parameter, χ2, Rp and Rwp of the GDC sintered at 1500(C for 10 h

| Sample | a-axis (Å) | χ2 | Rp (%) | Rwp (%) |
| --- | --- | --- | --- | --- |
| GDC | 5.4237(6) | 3.42 | 1.32 | 3.62 |

Standard deviation is shown in the bracket.

Table 3 Relative densities of the GDC sintered at 1500(C, 1000(C and GDC(composite prepared at 500(C

| Sample | Relative density (%) |
| --- | --- |
| GDC (1500(C) | 99.4(2) |
| GDC (1000(C) | 67.4(4) |
| GDC(composite | 99.6(2) |

Standard deviations are shown in the brackets.

Table 4 Conductivities, activation energies of the GDC and GDC(composite

| Sample | σ700 (mS·cm–1) | σ500 (mS·cm–1) | Ea (eV) | Temperature range ((C) |
| --- | --- | --- | --- | --- |
| GDC | 20.4(2) | 2.47(3) | 0.83(1) | 300(700 |
| GDC( composite | 144(4) | 104(2) | 1.04(5) 1.53(3) 0.22(1) | 300(425 425(500 500(700 |

Standard deviations are shown in the brackets.