具裂縫靜不定管結構的強制變位塑性行為解析

This paper study the plastic behavior of a cracked indeterminate pipeunder the forced displacement due to the vertical earthquake. Usingthe combination technique of limit analysis and elastic- plasticfracture mechanics to study the relation between J/sub IC/ and dJ/daso that the formation of the plastic hinge can be understood. Thenumerical results are plotted as the associated figures that can showthe plastic hinge, and crack growing much clear. The value of dJ/da isthe most effective factor to the deformation around the crack.