含磷紫外光硬化型環氧樹脂之合成

The object of this report is to synthesis the phosphorus-containingUV-curable epoxy resin. Generally the normal epoxy resin need muchtime to dry, so in this report we select the UV-curable type epoxyresin to applicate in more aspect. First, we use the AA (acrylic acid)to react to the epoxy resin to synthesis the UV-curable epoxy resin,then phosphorus pentaoxide add into the UV-curable epoxy/ THF solutionto synthesis our final product---phosphorus-containing UV-curableepoxy resin. The structure of this resin have the ability of chelatemetal. This resin might a new material of flameretardant anderoderesistance.