聚1,1-二氟乙烯摻合體的相形態結構與界面相容性之研究

Polyvinylidene fluoride (PVDF) was activated by plasma and modified by grafting of polystyrene (PS), which was characterized with FTIR and weighing method. The modified PVDF and polystyrene were employed to make solution blends, which were used in turn to prepare dense films by drying method. Electron microscopy was employed to study bi-continuous phases morphology of film. The thermal behavior and crystallinity were analyzed with DSC and XRD.