離胺酸的聚合反應

Lysine is an important amino acid, which is insoluble in most organic solvent. Solution of lysine in cosolvent of water/DMSO was prepared. Polymerization was conducted during the elimination of water by chemical or physical way. Different reaction parameters was studied to reveal the effect on the conversion as well as the degree of polymerization. The polylysine were characterized chemically by FTIR, NMR. Molecular weight was analyzed by EDI-MS, and thermal behavior by DSC.