無機鹽類添加物對薄膜結構之影響

The effects of inorganic salt (NaCl) on the morphology of Nylon66 membrane precipitated from water-formic acid solutions were investigated. It is found that Addition of NaCl into the dope increases the surface porosity and also the tendency formation of finger macrovoids in the membrane.