The Reactive Blend of PPS/PA12

This report presents a study of the relationship between morphology and chemical reaction of PPS/PAl2 reactive blends. Adding difunctional groups monomers (GMA, MAH) in PPS/PAl2 blends increases the reactivity of blends and produces more PPS-PAl2 block copolymers as compatibilizer. GMA monomers make PAl2 crosslink and this results in forming an additional second dispersed phase in PPS matrix. These evidences can be observed by the analyses of SEM and DSC.