硫化苯與耐龍6.6摻合的界面相容性反應與物性之分析

The modification of PA66 is firstly activated by plasma reaction andfollowed by the grafting of GMA. Then the modified PA66 with differentGMA grafting content is characterized and blended with PPS. Theincrease of interface adhesion is observed with FESEM due to theimprovement of compatibility between PPS and PA66 from in-situreaction of epoxide and thiol groups. Such evidence is revealedfurther form DSC, rheometric analysis.