H/sub 2/O-TEP-PVDF系統製作多孔型PVDF薄膜

Phase diagram of PVDF in water-TEP solutions was determined at 25℃.On the basis of the phase diagram, porous PVDF membranes were preparedby the immersion precipitation method. The porous structures of theformed membranes were observed in SEM. It was found that, dependingupon the preparation conditions, the membranes could assume eitherasymmetric or symmetric structures.